## Slide 1
Sensor on Foil platform
Matthias Simon, Walter Ruetten
Philips Research
February 9th, 2017
Gerwin Gelinck, Albert v. Breemen, Hylke Akkerman
Holst Centre/TNO
Jan Jacobs, Olivier Tousignant
Philips Healthcare

## Slide 2
Image sensors today1
Dominated by silicon based technology on rigid substrates
  High performance
  Large area applications difficult and/or expensive
  Rigidity hampers integration in products where form factor is important
  Mechanical integrity poor
CMOS sensor
Fingerprint sensor
Digital X-ray detectors
1 Market size estimated to reach USD 17.5 Billion by 2020
CAGR of 30% between 2015 and 2020

## Slide 3
Flexible image sensors
Can offer similar performance as compared to silicon, but:
  can be processed over large area, hence have a competitive cost per area ratio
  are thin and light weight
  are robust
  are conformable
  can be (semi)-transparent
Enable new products and product design

## Slide 4
Combination of new technologies for imagers
Oxide TFT backplane:
High electron mobility (20 cm2/Vs), low off current (<1pA)
Low process temperatures, compatible with plastic film substrates
Optically transparent
Organic Photodiode frontplane:
Effective light absorption from UV to near-IR
Low process temperatures, compatible with plastic film substrates
Competitive cost per area ratio

## Slide 5
Oxide transistor backplane on plastics
A key enabler of flexible electronics

## Slide 6
Oxide TFTs: semiconductor: InxGayZnzO (IGZO)
Etch stop layer (ESL) architecture
Flexible polyimide substrate
Processed on thin film barrier (optional)
Display fab compatible processes (at low temperature)
PECVD inorganic dielectrics
PVD metals (no noble metals)
PVD semiconductor (IGZO)
5 mask TFT process

## Slide 7
Organic photodiode (OPD)
Organic photoactive layer by slot-die coating: non-contact large-area blanket coating

## Slide 8
Organic photodiode (OPD)
-
Bottom electrode
D
A
Transparent top electrode
Light
Bulk heterojunction: mix of donor and acceptor material
High EQE
Low dark current

## Slide 9: Example: X-ray detector on foil
Wireless portable X-ray detectors are becoming more and more popular
  in mobile X-ray units  bed-side x-ray
  as replacement for fixed detectors in radiography rooms
Lighter and more robust detector
  will ease workflow for staff and patient
  less damage due to dropped detectors
Visions
  flexible X-ray detector -> wrap around body
  ‘ultra-mobile portable X-ray’
Wireless portable detector
Mobile X-ray unit
Trixell

## Slide 10: X-ray sensor on foil
Demo with image format VGA (480x640 pixel)
Area 6 x 8 cm2; pixel size 126 µm
Larger area in preparation

## Slide 11: Characterization with light and X-ray
CsI scintillator (400 µm) laid on
 X-ray image
Optical images

## Slide 12
Flexible sensors platform at Holst Centre

## Slide 13
Flexible sensors platform at Holst Centre

## Slide 14
Holst Centre

## Slide 15: Summary
18
Combination of different large area technologies
Foil-based imagers and X-ray detectors
Flexible sensor platform

## Slide 16: Research areas at Holst Centre
Structural
electronics
Solid state batteries
OLED
Lighting
Flexible
PV
Smart
windows
Smart clothing
Health patch
Flexible
displays
Flexible
imagers
Flexible
circuits
Large area
technology
Hybrid printed
technology
TFT technology