## Slide 1
Carlo Pepe1,2, Hobey Garrone1,2
Eugenio Monticone1, Mauro Rajteri1
(1)
(2)
INRiM work on calorimetry
6-7 October 2022 Zandvoort (NL)

## Slide 2
INRiM role in PTOLEMY
Target
RF
EM Filter
Microcalorimeter
Graphene
Monoatomic T storage
RF antenna
Measure of K and K⟂
Dynamic EM Filter
Particle selector
Calorimeter
TES provide a differential E measurement
KL
Is reduced arround few eV
18.6 kV
Microcalorimeter
Calorimeter
TES provide a differential E measurement
Andi Tan
(Princeton)
Notes: Più preciso su cosa lo rende un detector nelle varie applicazioni

## Slide 3
Calorimeter
C
G
ΔT
Tbath
Eγ
C = heat capacity
G = Thermal conductance
T=E/C
T
t
 = C/G
A Calorimeter is a device used to measure the change in temperature due to absorbed energy
Energy resolution
Sensor performance better at low temperature and with small C
Notes: Più preciso su cosa lo rende un detector nelle varie applicazioni

## Slide 4
Transition-Edge Sensors
Microcalorimeters based on the steep superconductive transition of a metallic film with:
  Excelent energy resolution
  Low dark count rates
  Near unit quantum efficiency
Measuring absorbed energy, it is sensible to:
  energy of a single particle
  number of particles
Applications:
  X-rays detection
  Telecommunications
  Quantum technologies
  Metrology
  Astrophysics
  Particle experiments
20 µm
Notes: Più preciso su cosa lo rende un detector nelle varie applicazioni

## Slide 5
How they work
ITES
PJ0
VOUT
Electrical circuit
Rbias<< RN
ITES
Ibias
Rbias
Lin
RTES
SQUID
Rfb
Lfb
Vout
voltage bias
Amplifier
TES is part of an electrothermal circuit and is operated in voltage bias mode (negative feedback).
The photons absorbed by the TES generate electrical signals that are readout through an inductance L coupled to a dc-SQUID used as transimpedance amplifier.
The amplitude of the impulse is proportional to the energy of the incident photons.
Vout
t
T
RTES
T
RTES (T)
0
RN
Bias point
RTES
RTES
Bias point
Electrical circuit
Rbias<< RN
ITES
Ibias
Rbias
Lin
RTES
SQUID
Rfb
Lfb
Vout
voltage bias
Amplifier
Notes: Voltage bias perché Rbias molto piccola.

## Slide 6
Amplitude (V)
time (μs)
0 20 40 60
0
-0.1
-0.2
1 γ
2 γ
0 γ
3 γ
How they works: detector features
Energy resolution
Effective response time
Critical temperature
Temperature sensitivity
Histogram of pulses amplitude for fixed photon energy
Saturation energy
The energy resolution improves for low TC

## Slide 7
TC tuning: proxymity effect
Ti
R (T)
0
RN
T
SiNX substrate
J. M. Martinis, G. C. Hilton, K. D. Irwin, and D. A. Wollman, “Calculation of Tc in a normal-superconductor bilayer using the microscopicbased Usadel theory,” Nucl. Instrum. Methods Phys. Res. Sect. A: Accel., Spectrometers, Detect. Assoc. Equip., vol. 444, no. 1/2, pp. 23–27, 2000
TC0
Varius
Fixed
Au
Au
Au

## Slide 8
INRiM Facilities: Fabrication
Laser writer
Sputtering Nb, Al technology
Thermal evaporation Au ,Ti
Up to 16 TESs per deposition
People:
Hobey Garrone (hobey.garrone@polito.it)
Eugenio Monticone
(e.monticone@inrim.it)

## Slide 9
INRiM Facilities : Measure
Adiabatic Demagnetization Refrigerator:
Base temperature down to 30 mK
Optical fiber integrated in the system
People:
Carlo Pepe
(carlo.pepe@polito.it)
Mauro Rajteri
(m.rajteri@inrim.it)

## Slide 10
INRiM Simulation of TES performances
H. Garrone, C. Pepe, A. Reineri, E. Monticone, R. Filippo and M. Rajteri, "Simulation software for transition-edge sensor performance prediction," in IEEE Transactions on Applied Superconductivity, doi: 10.1109 / TASC. 2022. 3146211.
https://tes.inrim.it/
INRiM online program:
Free access
TES performance simulations in the most established theoretical framesworks.

## Slide 11
INRiM TESs for PTOLEMY

## Slide 12
TES structure: Lito1 and Lito2
Nb
wiring
Thermal bath
Si
Ti 12 nm
Au 30 nm
SiNX 500 nm
SiNX 500 nm

## Slide 13
Lito1
Four terminal resistance measurement

## Slide 14
Lito2
Four terminal resistance measurement

## Slide 15
Photon counting characterization
baseline
min
Amplitude histogram
(baseline-min)
Counts
Amplitude
1 ph
0 ph
2 ph
3 ph
λ= 1540 nm
baseline
min
Counts
Amplitude
Amplitude histogram
avg(baseline)-min
0 ph
1 ph
2 ph
Laser trigger

## Slide 16
Lito1: T50
1
2
3
Histogram of pulses amplitude for fixed photon energy
50x50 µm (T50)
TC= 47 mK

## Slide 17
Lito2: T20
same result our APL13
but with an area
4 times greater
RTES= 20% RN
Tbath= 40 mK
λ = 1540 nm (0.8 eV)
20x20 µm (T20)

## Slide 18
Lito2: T20
RTES= 20% RN
Tbath= 40 mK
λ = 1540 nm (0.8 eV)
Saturation energy 12 eV

## Slide 19
Simulation resutls
Simulation for a squared TES with l x l area

## Slide 20
Q&A
The pressure in the deposition chamber was lower for Lito2, we resulting in a better quality of Titanium and its properties
Lito1 deteriorate in time losing the SC properties. Probably due the lower deposition quality
The Nb wiring has a proximity effect on the small TESs. This effect affect the small TESs more than the larger one
Lito1 and Lito2 have the same structure but different TC, why?
Why smaller TES of Lito1 were not measured considering the simulation?
Why in both Lito1 and Lito2 the transition of T10 TESs are not sharp as the larger TESs?
Questions
Answers

## Slide 21
Annealing
Tune the TC in the range of 50-70 mK is challenging working only on Ti/Au thinknesses
It Has been shown that thermal annealing can be used to have a fine tune of the TC in a Ti/Au bilayer
Van Der Heijden, N. J., et al. "Diffusion behaviour in superconducting Ti/Au bilayers for SAFARI TES detectors." Journal of Low Temperature Physics 176.3 (2014): 370-375.
Ti/Au strip1
Ti/Au strip2
Before annealing
After annealing
Thermal annealing at 130°C

## Slide 22
Summary
TiAu TES with TC < 100 mK fabricated.
First characterization with 0.8 eV photons
Best results up to now: E=0.114 eV @ Tc~ 90 mK T20
Results
Reduce the effect of wiring proximity effect using Ti instead of Nb.
Further test of the effect of the annealing to fine tune the TC of the TESs
It is time to work on the detection of electron with TESs:
  Cryogenic e-gun
  First characterization of TESs with keV electron?
Further investigation

## Slide 23
Carlo Pepe1,2, Hobey Garrone1,2
Eugenio Monticone1, Mauro Rajteri1
(1)
(2)
Thank you for the attention
6-7 October 2022 Zandvoort (NL)

## Slide 24
Discussion

## Slide 25
Backup slide

## Slide 26
Trade-off between response time and energy resolution
Effective response time
Energy resolution
TES: Performances
Saturation Energy

Trade-off between energy resolution and saturation energy

Transition sharpness

39 meV

## Slide 27
Amplitude (V)
time (μs)
0 20 40 60
0
-0.1
-0.2
1 γ
2 γ
0 γ
3 γ
How they works: equations and results
Energy resolution
Effective response time
Temperature variation
INRiM BEST ENERGY RESOLUTION
Temperature sensitivity

## Slide 28
TES behaviour
RESPONSE vs BIAS
0
200
400
600
Amplitude (mV)
400
800
1600
λ (nm)
1500
3000
4500
Counts
Saturation energy
TES behaviour depend on the working point, i.e. bias current, and on the wavelength of the incident particles.
TES saturation energy depend on TES properties only.

## Slide 29
TES polarization curve
Superconductive
Normal
77 mK
IBIAS (μA)
Working point
IBias=7.7 µA
R0=5% Rn
ITES (μA)
30
20
40
10
0
Rn =0.4 Ω
Electrical circuit
Rbias<< RN
ITES
Ibias
Rbias
Lin
RTES
SQUID
Rfb
Lfb
Vout
voltage bias
Amplifier

## Slide 30
Simulation resutls
Saturation energy  4 keV