## Slide 1
Silicon Sensor Development: Thin, Precise, Fast
Håkan Wennlöf on behalf of the Detector R&D team
20/5 -25

## Slide 2
Outline
Future colliders
Particle tracking
Silicon sensors
Work on monolithic prototypes
Simulations
Summary and conclusions

## Slide 3
Future colliders in particle physics
The next machine likely a lepton or lepton-hadron collider (ECFA Raodmap, 2021)
  Adding precision measurements of e.g. the Higgs boson
  Addressing questions within the standard model
  Providing sensitivity to new physics
Leads to strict precision requirements in time and space

## Slide 4
Particle tracking – why?
Studying particles in detail requires interactions
  Frequently achieved by smashing particles together
Tracking of individual resulting components is needed for reconstruction
  Gives information of e.g. momentum and interaction position for collision products
  Crucial for determining underlying physics processes
https://commons.wikimedia.org/wiki/File:Lorentz_force_on_charged_particles_in_bubble_chamber_-_HD.6D.635_%2812000265314%29.svg
https://cds.cern.ch/record/39444

## Slide 5
Particle tracking in practice
Requires large detector area and fine granularity to get the most information
  Several layers of high-granularity detectors
Inner layers need superb precision – down to a few µm
Large area to be covered (tens of m2) – silicon is a natural choice
  Small pixel sizes
  Relatively cheap to produce large areas
https://cds.cern.ch/record/1625842
Inner Tracking System
49 eurocents

## Slide 6
Particle tracking in practice - future
Higher precision needed
  Smaller pixel sizes and less material – reduce scattering
Higher track densities
  Requires radiation hardness
  Better temporal resolution to reduce pile-up effect
    Separate tracks in time - “4D tracking”
2 ns
Fast timing
© LHCb Collaboration

## Slide 7
Silicon sensors
Silicon is a semiconductor
Through interaction with ionising radiation, electron-hole pairs are freed
The motion of electron-hole pairs within the sensor gives rise to our signal
Both radiation hardness and fast timing demands faster charge collection and more sophisticated front-end electronics
Traversing particle
e-
e-
e-
e-
e-
e-
e-
h+
h+
h+
h+
h+
h+
h+
Signal
Front-end electronics

## Slide 8
Fast Timing group work
Working at the forefront of silicon sensor development
Significant involvement in the Timepix project – see e.g. last jamboree
  Sophisticated front-end chip, providing excellent time resolution
Many different sensors tested
  Internal charge multiplication: different types of low-gain avalanche diodes
  3D sensors of different geometries
Monolithic sensors

## Slide 9
Fast Timing group work
Working at the forefront of silicon sensor development
Significant involvement in the Timepix project – see e.g. last jamboree
  Sophisticated front-end chip, providing excellent time resolution
Many different sensors tested
  Internal charge multiplication: different types of low-gain avalanche diodes
  3D sensors of different geometries
Monolithic sensors

## Slide 10
Monolithic sensors
Combines sensitive volume and front-end electronics in a single wafer
  Simplified production
  Allows smaller pixel sizes and thinner detectors
    Beneficial for spatial and momentum resolution
If silicon gets thin enough, it bends
Issues:
  Difficult to optimise – electronics have to be more compact and limited
  Production details proprietary
ITS3 Engineering Model 1

## Slide 11
Monolithic prototypes at Nikhef
State-of-the-art sensor prototypes available at Nikhef
Focus on two, developed in the frame of the ALICE experiment:
  Monolithic Stitched sensor with Timing (MOST)
  Analogue Pixel Test Structure (APTS)
Need thorough testing and characterisation
  Do they function as intended?
  Can possible improvements be found?
https://indico.cern.ch/event/1386009/contributions/6279104/

## Slide 12
The MOST prototype
Stitched sensor with a very dense matrix
  Sophisticated electronics in a new technology
Studying production quality
  How many sensors are functional?
  How many pixels respond as expected?
Also studying time performance – jitter between input signal and chip output
  Sergei performing thorough studies of this
Jitter measurement
Preliminary

## Slide 13
APTS work - strontium-90
Want to find the time response of the sensor under different conditions
Tabletop setup built
  Using a beta source to get an electron “beam”
  Cherenkov radiators and photon detectors sandwich the sensor to get a trigger signal
Allows on-site testing of sensor temporal resolution
  Jaïr currently studying irradiated APTS sensors
https://scripties.uba.uva.nl/search?id=record_55356

## Slide 14
APTS work – laser measurements
Investigating the response versus interaction position
  Using a pulsed infrared laser with precision motion stages
Can correlate hit position to sensor response
  Generating maps of e.g. signal amplitude and temporal behaviour
Esther currently working on this for the APTS, and Artem, Mariia, and Sergei for the MOST
y (µm)
x (µm)
Sensor current
Laser driver
Optical fibers
Motion stage
Chip board

## Slide 15
APTS work - testbeam
Using a particle beam provided e.g. at the CERN SPS
  Allows testing in experiment-like conditions
Device under test (DUT) mounted in beam along with reference system
  Allows knowledge of where and when a particle traversed the DUT
    Can match DUT signal to interaction position and time
  Provides measurement of detection efficiency
Isis working on analysis of data from a testbeam in October 2024

## Slide 16
Simulations
Used to further understanding and investigate new designs
Invaluable tool for both detailed and intuitive understanding of sensor behaviour
Combination of detailed finite-element method solvers for internal electric field, and fast Monte Carlo simulations for high statistics
Doping profile
Electric field

## Slide 17
Allpix Squared – Monte Carlo framework
Allows detailed simulation of full pixel hit chain in a semiconductor
  From particle interactions to front-end electronics treatment of signal
Open-source, based on a modular design, written in modern C++
Fast; gives access to high statistics simulation of signal generation steps in a pixellated sensor
Can be used for both quick investigations and highly detailed simulation studies

## Slide 18
Allpix Squared
Enables simulation of charge carrier transport within a sensor
Example: electrons and holes propagating in a linear electric field and constant magnetic field
  Note: electrons move faster than holes in silicon
Can visualise and understand where observed features come from
■ electrons
■ holes
E
B
Traversing particle

## Slide 19
Allpix Squared
Enables simulation of charge carrier transport within a sensor
Example: electrons and holes propagating in a linear electric field and constant magnetic field
  Note: electrons move faster than holes in silicon
Can visualise and understand where observed features come from
■ electrons
■ holes
E
B
Traversing particle

## Slide 20
Allpix Squared – microscopic simulations give macroscopic effects
A good match to data is found, enabling predictive simulations
Highly detailed in-pixel studies can be performed
A. Simancas et al. doi:10.1016/j.nima.2024.169414
doi:10.1016/j.nima.2025.170227

## Slide 21
Summary and conclusions
High precision in both time and space essential for experiments at future colliders
  Silicon detectors can meet many of the demands
There is a lot of activity in the Detector R&D group targeted at future experiments
  Working at the forefront of silicon sensor development
  Investigating several new technologies
Prototype testing and simulations together make a powerful toolbox for sensor research and development – we do both at Nikhef!

## Slide 22
Thank you!

## Slide 23
Backup slides

## Slide 24
MAPS prototype timing status
Time resolution for APTS measured for different radiation damage levels
  63-69 ps across full pixel
For MOST, the jitter of on-chip signal propagation has been measured
  Down to tens of ps

## Slide 25
APTS timing status
Strong dependence on in-pixel position
Time resolution in pixel centre lowest
  51-63 ps
Slower at pixel edges – charge travels for longer before inducing a charge

## Slide 26
LGAD simulations for ALTAS HGTD
Simulating particle incidence on low-gain avalanche diode
Pulse generated by charge motion and amplification
Sophisticated front-end electronics response included via transfer function
Work by Petja

## Slide 27
Full end-to-end simulations – only Allpix Squared
Signal
Transfer
Digitization
Charge
Transport
Energy
Deposition
incident radiation
e-
e-
e-
e-
e-
e-
e-
e-
e-
h
h
h
h
h
AC/DC
0111010010100101
detector readout
x
t
h
h
h
h
h
e-
Spannagel et al, 2018
Dannheim et al, 2020 Spannagel et al, 2022
Wennlöf et al, 2025

## Slide 28
Combining tools for full end-to-end simulations
Signal
Transfer
Digitization
Charge
Transport
Energy
Deposition
incident radiation
e-
e-
e-
e-
e-
e-
e-
e-
e-
h
h
h
h
h
AC/DC
0111010010100101
detector readout
x
t
h
h
h
h
h
e-
Spectre Simulation
Sentaurus TCAD
HepMC3
CRY Cosmic Ray Showers
ATLAS TCAD
Spannagel et al, 2018
Dannheim et al, 2020 Spannagel et al, 2022
Wennlöf et al, 2025

## Slide 29
Single particle traversing monolithic silicon sensor, simulated using Geant4
  Energy deposits along particle track
Electric field and doping concentration imported from TCAD in the green region
Charge carriers propagated primarily by diffusion in grey region, and drift in green region
Simulation example
■ electrons
■ holes
pixel boundary
MIP path
collection electrodes

## Slide 30
Complexity of detectors increases, more and more technologies available,
different approaches combined (e.g. monolithic + LGAD)
  Necessity of MC simulations growing
  Some sensors / setups impractical to simulate in TCAD (time limitation, stochastics)
  Community needs common flexible, tested & supported MC simulation tools
Using Monte Carlo methods to describe detector response is not new
Creation & proliferation of many different codes for detector simulation
  Experiment-specific
  Specialized on specific detectors
  Inclusion only of effects relevant to that one simulation
  Written as part of a PhD thesis, abandoned afterwards
Would be great to collate features in commonly maintained software (->SM)
  Having several tools is valuable as testbed for algorithms
  Well-maintained & supported common software will significantly ease use in community
Semiconductor Detector MC Simulations
Community Meeting 22-23/03/2023
Implementation of TF3
Solid State Detectors