## Slide 1: The next best vertex detector at the LHC
Kazuyoshi CARVALHO AKIBA

## Slide 2: Self Introduction
Velo Controls+DAQ
Velo Commissioning & optimization of raw data
Currently at UFRJ: Adj. Professor (2011-)
  Coordinator of the local HEP lab
  Teaching: Nucl. Phys. Lab & Instr. lab
  Deputy Project leader of the VELO (2014-)
  CERN SASS (2014-2015)
  Test beam coordinator (2015-)
  Main research – VELO upgrade
Side projects/interests:
  Co-proponent of applied physics programme in UFRJ
  Medical physics (eye tumour irradiation)
  X-rays at the Brazilian Synchrotron
  Herschel (FSC for diffractive pp interactions)
Grants:
  Local lab infrastructure: Si R&D measurements
  Construction of a Pixel Telescope
  +Personal grants
2006
2014
2005
2007
2008
2011
2014
2016

## Slide 3: Quick Recap
Contains
1 Velo half
RF-Foil
LHC RUN I | Delivered Luminosity | Highest Fluence*
CMS pixel | ~29.5 fb-1 | 9x1013 1MeV neq/cm2 At 39 mm
VELO | ~3.4 fb-1 | 17x1013 MeV neq/cm2 At 8 mm
42 Double sided
@1 MHz
4 single sided
@ 40 MHz
Non uniform irradiation
profile

## Slide 4: How to improve the Vertex Locator?
Go closer to the collisions
Minimise the material
Improve hit resolution
Read more collisions at once

## Slide 5: VELO Upgrade
Upgrade detector: hybrid pixel technology
Current detector: strip technology
42 shaped double sided modules (R/f)
84 sensors.
52 L shaped modules
208 sensors.
Challenge: Read out every hit at 40 (30) MHz crossing rate
All events to computing farm: Fast pattern recognition in the trigger
Higher occupancy bigger granularity.

## Slide 6: From strips to hybrid pixels

## Slide 7: Sensors
1%
The Velo sensors must collect: 6000e-/MIP – 99% eff. at 370 MRad8 x 1015 1 MeV neq/cm2. this is equivalent to 50fb-1 @LHCb_up
  The ATLAS IBL – at 550 fb-1 – expects 3.3 x 10151 MeV neq/cm2 or 160 MRad.
Radiation hardness was never proved for such small pixels: 55x55 mm .
  ATLAS  50x250 mm (FE-I4)
Irradiation tests are mandatory Particular for the VELO: non uniform irrad.
Collection time – Could change after irradiation
Longer pixels
~43mm
ASIC
Sensor tile
sensor
ASIC
ASIC
Put together by bump bonding
100%

## Slide 8: VeloPix
Binary readout
25 ns Time stamping
Extreme data rate
  800 Mhits/s
  20 Gbit/s output bandwidth
SEU robust
TSMC – 130 nm
The final chips will be thinned
14.14 mm
Analog front-end
16 x 55 um²
Pixel & Superpixel

## Slide 9: Thinning and bumping
To minimise material, ASICs will be thinned to 200 mm
ASICs and sensors must be metallised before receiving solder bumps
During reflow, this could lead to bowing due to metal layers in the chip.
2 companies trying to provide a reliable method

## Slide 10: Thinning and bumping
To minimise material, ASICs will be thinned to 200 mm
ASICs and sensors must be metallised before receiving solder bumps
During reflow, this could lead to bowing due to metal layers in the chip.
2 companies trying to provide a reliable method

## Slide 11: Sensor Prototypes
Micron
HPK
Round 1 HPK (CERN-Rio-USC):
  N-on-p 200 mm thick
  450 and 600 mm PTE
  35 and 39 mm implant
  UBM
Micron (L’pool):
  N-on-n and n-on-p
  36 mm implant
  150, 250 and 450 mm PTE

## Slide 12: Sensor Prototypes
Micron
HPK
Round 1 HPK (CERN-Rio-USC):
  N-on-p 200 mm thick
  450 and 600 mm PTE
  35 and 39 mm implant
  UBM
Round 2 HPK (Rio):
  39 mm implant, 450
  Rounded corners
Micron (L’pool):
  N-on-n and n-on-p
  36 mm implant
  150, 250 and 450 mm PTE

## Slide 13: How to decide?
Needs to fully test before and after irradiation
HV Tolerance – systematic testing of many assemblies
Charge collection – requires calibration methods
Resolution – requires track reconstruction
Drift time – requires precise track time measurement

## Slide 14: Irradiation Programme
If we have control over the collected charge we can study it as function of fluence.
Used a few different facilities:
KIT, IRRAD, JSI, IST Birmingham
Special focus on non-uniform irradiation.
IRRAD @ CERN 24 GeV p.
KIT @ Karlsruhe 24 MeV p

## Slide 15: Irradiation Programme
If we have control over the collected charge we can study it as function of fluence.
Used a few different facilities:
KIT, IRRAD, JSI, IST Birmingham
Special focus on non-uniform irradiation.
IRRAD @ CERN 24 GeV p.
KIT @ Karlsruhe 24 MeV p

## Slide 16: HV Tolerance
HPK non-irrad
HPK KIT irrad
Non uniform
Non parylene
Sensors tested in vacuum.

## Slide 17: Sparking

## Slide 18: Parylene
Contacted SCS coatings (USA) and Comelec (swiss)
Parylene is deposited in all surfaces exposed.
Chips are placed in vacuum, at high temperature.
Masks are applied to the chips prior to deposition.

## Slide 19: Parylene problems
Problems encountered with “low” energy high intensity proton beam (24 MeV), but only on non-uniform irradiation.
Increased noise in chip seemed to be mitigated by Ikrum.

## Slide 20: Charge collection
VeloPix was not ready when the sensor R&D was performed
Used Timepix3 for the studies
Several testing methods were employed before the SPS beam was back (<2014)
  Sr90
  Am241
  Synchrotron X-rays
Extensive beam studies carried out

## Slide 21: Charge calibration
Calibrated per pixel using test pulses
Test pulse
Per pixel fit
p1 - Slope

## Slide 22: Charge calibration
Cross checked with known x-ray lines
Am 241 per pixel fit
Test pulse
Per pixel fit
Am 241 spectrum all pixels
Non-clustered
Clustered
Am241 uncalibrated

## Slide 23: Charge calibration
Cross checked with known x-ray lines
Am 241 per pixel fit
Test pulse
Per pixel fit
Am 241 spectrum all pixels

## Slide 24: Charge calibration: LNLS*/Campinas
XAFS1 - X-ray Absorption and Fluorescence Spectroscopy
4 to 24 keV photons with sE/E~ 0.01%.
*National Synchrotron Light Lab

## Slide 25: Charge calibration: LNLS*/Campinas
*National Synchrotron Light Lab

## Slide 26: Testing prototypes with beam
Using Timepix3 as VeloPix prototype
4 Timepix3 on 2 “arms”
Charge measurement and clustering yields a 2 mm pointing resolution.
Precise time stamps (1.56 ns) make it simple and clean for the Pat. Rec.
We have operated up to 5 Mtracks/s/cm2.
Picture of the Timepix3 telescope, at CERN SPS
DUT
Beam
Planes
Readout electronics
Pointing resolution

## Slide 27: What if we didn’t have the beam at CERN?
In 2012 we knew that there would be no beam at CERN till mid 2014…
What if we would like to go to Fermilab? DESY?

## Slide 28: COMpact BrAzilian Telescope
Motivation
  To be portable, by airplane
  As good as the Timepix telescope, if not better.
  “Easy” to be put together
  Low cost.
stages

## Slide 29: COMBAT construction
CLIC sensors. 8x150 mm thick sensors on 4x150mm and 4x700mm TPX chips.
3D printed detector holders at 20o for optimal charge sharing
PCB cut out under the sensor – less material.
5.1 mm
Taking data at SPS – 2014

## Slide 30: COMBAT Readout
0
1
2
3
RELAXD0
DAQ PC
4
5
6
7
RELAXD1
Dual RELAXD readout
  backup plan
Pre-commissioned with cosmics
Created custom readout with a PXI Flex-RIO 7952 board (Virtex5) for 9 planes

## Slide 31: COMBAT Readout
Dual RELAXD readout
  backup plan
Pre-commissioned with cosmics
Created custom readout with a PXI Flex-RIO 7952 board (Virtex5) for 9 planes
  Ready in 2015

## Slide 32: Back to Sensor R&D results

## Slide 33: Hit resolution
  HPK 200 µm n-on-p
  Micron 200 µm n-on-p
  Micron 150 µm n-on-n
Best resolutions just below 5 µm.
Charge weighted – Non Binary data.
Non irradiated sensors
Irradiated sensors

## Slide 34: Charge Collection – Non Irrad

## Slide 35: Collected Charge – IRRAD
JSI irradiated sensors
  HPK 200 µm n-on-p
  39 µm

## Slide 36: Timing
Different amplitude and same threshold could lead to time walk:
t0 t1 t2
Th

## Slide 37: Timing
Different amplitude and same threshold could lead to time walk:
t0 t1 t2
Th
Combined track resolution: 350 ps.
Average time of each telescope station

## Slide 38: Timing
Different amplitude and same threshold could lead to time walk:
For the VeloPix, all the hits should be inside 25 ns .
Time to threshold
amplitude
Time between hit and track
t0 t1 t2
Th
Hit time
residual: s = 1ns
25 ns limit
Combined track resolution: 350 ps.
Average time of each telescope station
HPK, parylene coated non-irrad

## Slide 39: Timing
Different amplitude and same threshold could lead to time walk:
For the VeloPix, all the hits should be inside 25 ns .
amplitude
Time between hit and track
t0 t1 t2
Th
25 ns limit
Combined track resolution: 350 ps.
HPK, parylene coated non-irrad
HPK, parylene coated neutrons - full fluence
Average time of each telescope station

## Slide 40: Timing
Different amplitude and same threshold could lead to time walk:
For the VeloPix, all the hits should be inside 25 ns .
amplitude
Time between hit and track
t0 t1 t2
Th
Average time of each telescope station
25 ns limit
Combined track resolution: 350 ps.
HPK, parylene coated non-irrad
HPK, parylene coated neutrons - full fluence

## Slide 41: Timing excursion – VELO – 2009
Width 1
Width 2
Amplitude
Peak (ns)
Constant
(offset)
Spillover (ns)
Fix values based on known pulse shape

## Slide 42: Velo Timing resolution – 2009

## Slide 43: Velopix Timewalk measurements
Performing Velopix Timewalk tests with SPIDR and Test pulses

## Slide 44: Velopix Timewalk measurements
Check measurements as function of temperature: VELO operates @ -20oC Tests to be made in dry air or vacuum.
Laser setup: 10 ns pulse, 12 um spot 660nm, 1060nm wavelengths

## Slide 45: Summary
R&D for the VELO upgrade sensors is concluded: Moving onto production.
Constructed a rival tracking system in Brazil.
VeloPix + controls & DAQ testing will be the focus in the next test beams.
Testing of thinned chip assemblies to validate the production.
VeloPix cooled time walk to be measured in the lab.
Timing measurements are the coolest thing since

## Slide 46: Bedankt

## Slide 47: Backup

## Slide 48: Upgrade Modules
2 sensor tiles + ASICS on
each side of the module
Micro channels etched
in silicon to bring
liquid CO2 under the chips.
Low material active cooling.
Electronic hybrids to be attached to cooling substrate.
Controls and read out

## Slide 49: Fluorescence MPX3 Measurements

## Slide 50: Intra pixel efficiency
D.Saunders
At 1000 V the corners are recovered.
36 mm n-on-n
X[mm]
Y[mm]
S27
Micron
300V
HPK
Pixel centre
Pixel corner

## Slide 51: Collected Charge – JSI
JSI irradiated sensors
  HPK 200 µm n-on-p
  Micron 200 µm n-on-p
  Micron 150 µm n-on-n

## Slide 52: Hamamatsu IV tests
Check performed for each triple/single on guard ring only

## Slide 53: COMpact BrAzilian Telescope

## Slide 54: Time is the new Space
Time tags can isolate hits from the same track.
Tracks from the same PV have the same time.
An SV can be tagged to its PV by the same time!
Z  mm in 25 Collision event. HL-LHC can go to 10x that
But the hit precision must go below 100 ps
2mm spacing between vertices 200 mm
5 cm
Simple
hits
Timed
hits

## Slide 55: 4D Tracking – is it really necessary?
Tracking performance (no tuning)
  VELO upgrade: 99% efficiency, 2% ghosts
  At 10x luminosity: 94% efficiency, 42% ghosts
Track association to primary vertex
  VELO upgrade: 1% mis-association
  At 10x luminosity: 13% mis-association
    Degrades decay time resolution
4D tracking: add timing information
  Improves tracking performance
  PV mis-association vs. time resolution
    200 ps hit resolution could recover current Velo Upgrade performance
LHCb Unofficial
LHCb
Unofficial
Time resolution per hit [ps]
LHCb
Unofficial
PV mismatch [%]

## Slide 56: R&D on fast timing
200 mm sensor+ASIC+ mchan cooling
LGAD
N. Cartiglia, VCI 2016
LGAD CNM
NA62 Gigatracker: ~150 ps resolution, TDCPix.
Timepix4 plans 200 ps TDC.
Low Gain Avalanche (LGAD) technologies theoretically to achieve 20 ps
Giga tracker TDC Pix
simulations

## Slide 57: Timeline
year | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022+
beam crossing | 50 ns |  |  | LS1 |  | 25 ns |  |  |  | LS2 |  | 25 ns | 
TeV | 0.9 | 7 | 8 |  |  | 13-14 |  |  |  |  |  |  | 
Instant Luminosity | 1032cm-2s-1 | 3-4x1032cm-2s-1 |  |  |  | 4x1032cm-2s-1 |  |  |  |  |  | 2x1033cm-2s-1 | 
Integrated Luminosity | 3 fb-1 |  |  |  |  | 5 fb-1 |  |  |  |  |  | 50 fb-1 | 
Sensor production
module production
Assembly
installation
Current upgrade plan still compatible with post LS3 …
VELO
TDR
UT
TDR
LOI
FW
TDR

## Slide 58: Cooling: micro channel substrate
Challenge:
Modules produce up to 30W, dominated by ASICs
Sensors must be kept < -20 oC to minimize the effects of radiation damage, and to avoid thermal runaway
Must avoid material especially at tip of module
CO2
Race track design
simulations
Cross section of the module concept
Soldered connector
Chosen Solution:
Evaporate CO2 in micro-channels etched within silicon substrate
  High heat transfer coefficients
  No CTE difference (Si on Si)
  Excellent uniformity of material in sensitive region
  Pressure tolerance of module is important

## Slide 59: Microchannels under test
Nominal
Maximum
Power
Tested 2
samples
  Double Micro channel test setup
Cooling performs with very low DT and
well beyond necessary power

## Slide 60: Irradiated resolution
Charge weighted -- Non Binary data.
Binary like resolutions
  HPK 200 µm n-on-p
  Micron 200 µm n-on-p
  Micron 150 µm n-on-n

## Slide 61: Timepix3 – charge measurement
The calibration of the charge measurement has to be well understood, in order to compare different prototypes, and also at various irradiation levels.
M.Williams
M.Vicente
Am241 spectrum
Timepix3 is the ideal tool: very precise and easy charge collection measurement
  Timepix(1) is not radiation hard.
  Medipix3 requires slow (tedious) threshold scans
  Velopix is not out. And it’s binary.
But requires tuning and calibration.

## Slide 62: The Telescope – our infrastructure.
R.Dumps
No significant loss
Correlated to rate.
A.DosilSuarez
The Timepix3 telescope is fast, precise, and easy to combine with Timepix3 DUTs.
The software is written in Gaudi architecture: Kepler. ~15k tracks/s.
Charge measurement and clustering give a great pointing resolution down to 2 mm.
Precise time stamps make it simple and clean for the PatRec.
Tracks can be measured with 0.4 ns timing precision
We have operated up to 10 Mtracks/s/cm2.

## Slide 63: Collected Charge
JSI irradiated sensors
  HPK 200 µm n-on-p
  Micron 200 µm n-on-p
  Micron 150 µm n-on-n

## Slide 64: Efficiencies for irradiated sensors
Uniformly
Irradiated sensors
To full fluence.
Recovered corners
At 1000V bias.

## Slide 65: Efficiencies for irradiated sensors
Uniformly
Irradiated sensors
To full fluence.
Inefficient corners
At 500V bias.

## Slide 66: Efficiency
The crucial part of the efficiency measurement is selecting the right tracks…
A careful clean-up removing nuclear interactions, dead pixels, noisy and vertices is performed.
Also 20 ns Dt cut..
DUT
D.Saunders

## Slide 67: Edge Analysis
Charge and clusters accumulate in the
First (busiest) column
 VeloPix won’t cope (higher hit rate) worse resolution
E.Dall’Occo

## Slide 68: Edge Analysis
S20
HPK
200V
S23
Micron
200V
(n-on-p)
S30
Micron
200V
(n-on-n)
E.Dall’Occo

## Slide 69: Edge Analysis
S20
HPK
200V
S23
Micron
200V
(n-on-p)
S30
Micron
200V
(n-on-n)
E.Dall’Occo
S23 n-on-p irradiated
900V

## Slide 70: Edge Noise – after irradiation.
We have observed
noise clusters at the edge In a irradiated n-on-n
Micron Irradiated with neutrons (JSI)
Seems to get better
increasing the pre-amp
Discharge current (Ikrum)
Under investigation!
And cross checking
If we see it in any of
HPK sensors.
V.FrancoLima

## Slide 71: Grazing Angle
An alternative method that provides interesting results!
H.Snoek, P.Tsopelas
Non-irradiated HPK
Irrradiated
HPK
dE/dx for 55 mm of silicon Q = 3.8 ke

## Slide 72: VELO Gain, timing, signal calibration
Proton
Kaon
Electron
Pion
Separation only below 2 GeV

## Slide 73: One Picture every 25 ns
40 million events* per second at the LHC
20-50 Tracks per collision
*LHC bunch crossing frequency of ~30 MHz (2808/3654 filling), but more than more than 1 collision is possible/likely
Notes: Driving motivation to allow physics discoveries in human life times is given by two main factors, much higher statistical samples and precision in each measured event.

## Slide 74: Decay time resolution
A data driven approach compares the decay vertex with reconstructed candidates with the same topology. In this case Bs->J/yf.
The MC simulation compares the reconstructed position with the generated one.

## Slide 75: B0s oscillations and Dms in LHCb
Also D0 oscillations:
Phys. Rev. Lett. 110, 101802 (2013)
Decay time resolution depends on the channel, for the one used (BsDsp): 44 fs.
The main systematic error is on the length scale of the VELO: 4 fs-1.
First measurement with 36 pb-1 (2010 data): Phys.Lett. B 709 (2012) 177-184
Result with 1 fb-1 (2013)

## Slide 76: Hit resolution
Hit Resolution as function of track angle
 Varies from 10 to 30% of the pitch
Hit Resolution can go as low as 4 mm
Use the detector as a telescope to study unbiased resolutions

## Slide 77: Monolithic Active Pixel Senors
Thinner, more segmented and smart detectors.
Advantages:
  Industry friendly
  No bump bonding/flip chip
  Can be very thin O(50 mm)
  Can have on pixel amplification
  Possibility to use new inter- connections (e.g. CCPDs)
Disadvantages:
  Collection mostly by diffusion (slow).
  Traditional (imaging-like) technology is not radiation hard (~1013 neq)

## Slide 78: HV (HR)-CMOS
Ideally one would like to achieve:
  Low capacitance – low power
  Good S/N
  Good time resolution
  High rate capability
  Radiation tolerance
  Single sided processing: low cost mass production
P substrate
depletion layer
N well
-85V
~9μm
One deep n-type well in a p-type substrate acts as a collecting electrode.
Reverse bias between n and p-types increases the depletion volume.
Low resistivity (HV)  radiation hard

## Slide 79: HV (HR)-CMOS
P substrate
depletion layer
N well
-85V
~9μm
Complex CMOS electronics can be built inside the n-well.
Small pixels ~20 mm can be achieved.
Thin volumes will help keeping a low cluster size.
This is being developed for m3e and ATLAS ITK.
One deep n-type well in a p-type substrate acts as a collecting electrode.
Reverse bias between n and p-types increases the depletion volume.
Low resistivity (HV)  radiation hard

## Slide 80: HV (HR)-CMOS, m3e example
  Spatial resolutions of ~20 μm were reached with pixels of 103 x 80 μm2.
  Further improvement can be reached with smaller pixel sizes.
MuPix7 chip
  Good time resolution could be achieved thanks to Biasing voltage

## Slide 81: Radiation hardness of MAPS?
Still to be achieved… but:
C.J.S. Damerell, 1995
VERTEX DETECTORS: THE STATE OF THE ART AND FUTURE PROSPECTS

## Slide 82: Motivated by physics
Some particles “live” longer than others (b and c hadrons)
The shorter they live the harder it is to separate them from the collision point.
Precise measurements of the collision and displaced vertices, allow a wide range of physics observations
  CP violation, rare decays
  Higgsbb, bb resonances
  particle oscillations
  New particles
*S Tsuno, Pixel2016
2 out of 3 ATLAS analyses use b jet information, as presented in ICHEP 2016
N/A (35.2%)(*)
(*) Of course still use some level of vertex and tracking
N =1 (20.4%)
bjet
Nbjet=2 (16.7%)
Nbjet>- 3 (9.3%)
Nbjet=0 (9.3%)
top CR (9.3%)
Notes: The purpose of a vertex detector is to measure position and angles of charged particle tracks to sufficient precision so as to be able to separate tracks originating from decay vertices from those produced at the interaction vertex.
Such measurements are interesting because they permit the detection of weakly decaying particles with lifetimes down to 10-13s, like charm and b hadrons

## Slide 83: Key physical parameter
Excellent impact parameter resolution is mandatory for reconstruction of heavy flavour vertices.
Secondary vertex reconstruction depends on impact parameter (IP) resolution
d0
PV
SV
Notes: Many Tracks contribute to the primary vertex reconstruction. Secondary vertices are displaced from those

## Slide 84: Detector Constraints
Impact parameter resolution depends on 3 main parameters
  Intrinsic hit resolution
  Distance to the first measured point and lever arm
r1
r2
d0
s1
s2
2 point measurement

## Slide 85: Detector Constraints
Impact parameter resolution depends on 3 main parameters
  Intrinsic hit resolution
  Distance to the first measured point and lever arm
  Multiple scattering in detector material, (worse at low pT)
r1
r2
d0
s1
s2
2 point measurement
q
x
Multiple scattering

## Slide 86: Detector Constraints
Impact parameter resolution depends on 3 main parameters
  Intrinsic hit resolution
  Distance to the first measured point and lever arm
  Multiple scattering in detector material, (worse at low pT)
r1
r2
d0
s1
s2
2 point measurement
q
x
Multiple scattering

## Slide 87: High Energy Physicist wish list
Good Primary Vertex resolution – separate between collisions.
Good Impact Parameter resolution – isolate particles from primary to secondary vertices.
Good Secondary Vertex resolution – to precisely measure long lived particles.
This implies:
  Good hit resolution – small size detection elements.
  Get close to collision point – high radiation environments.
  Low material – thin sensors of low density.

## Slide 88: VELO Performance

## Slide 89: Primary vertex resolutions
Parametrised as A/(Ntracks)B + C

## Slide 90: Impact parameter resolution
d0 res. as function of p
d0 res. as function of 1/pT
Compared to the other LHC experiments

## Slide 91: The LHCb Vertex Locator (VELO):
88 silicon
sensors
R-φ design
300 μm, n+n Si
2048 strips
ractive = 8.2mm
pitchmin = 40 μm
Moves away every fill and
centers around the beam with self measured vertices

## Slide 92: The LHCb Vertex Locator (VELO):
Separated from primary vacuum by thin RF foil with complex shape – Protection from beam pickup
Operates in vacuum
88 silicon
sensors
R-φ design
300 μm, n+n Si
2048 strips
ractive = 8.2mm
pitchmin = 40 μm
Moves away every fill and
centers around the beam with self measured vertices

## Slide 93: The LHCb Vertex Locator (VELO):
Operates in vacuum
88 silicon
sensors
R-φ design
300 μm, n+n Si
2048 strips
ractive = 8.2mm
pitchmin = 40 μm
Evaporation of CO2 keeps the temperature stable.
CO2
Separated from primary vacuum by thin RF foil with complex shape – Protection from beam pickup
Moves away every fill and
centers around the beam with self measured vertices

## Slide 94: The LHCb Vertex Locator (VELO):
Operates in vacuum
88 silicon
sensors
R-φ design
300 μm, n+n Si
2048 strips
ractive = 8.2mm
pitchmin = 40 μm
Evaporation of CO2 keeps the temperature stable.
CO2
LHC RUN I | Delivered Luminosity | Highest Fluence* per fb-1
CMS pixel | ~29.5 fb-1 | 3x1012 1MeV neq/cm2 At 39 mm
VELO | ~3.4 fb-1 | 5x1013 MeV neq/cm2 At 8 mm
Separated from primary vacuum by thin RF foil with complex shape – Protection from beam pickup
Moves away every fill and
centers around the beam with self measured vertices
Radiation exposure